## Slide 1
Lesson 1
Wood properties, its limitations and wood construction physics
LEARNING UNIT 1:

## Slide 2
Presentation Overview
- Wood structure and appearance
- Physical properties
- Mechanical properties
- Technological properties
- Operational properties
TOPICS DISCUSSED
LESSON 1: Wood properties, its limitations and wood construction physics

## Slide 3
WOOD STRUCTURE AND APPEARANCE
1/2
3
LESSON 1: Wood properties, its limitations and wood construction physics
Micro and macro structure
How it can be used
Wood welding
(click on the picture)
https://www.twi-global.com/media-and-events/press-releases/2019/twi-develops-wood-welding-process
Theapparat and Chandumpai, Physicochemistry and Utilization of Wood Vinegar from Carbonization of Tropical Biomass Waste. 2018
Hodley R.B. Understanding Wood: A Craftsman's Guide to Wood Technology. 2000
Wertheimer D. Moisture & Wood Movement. How To & Calculators, 2019
Timber cuts

## Slide 4
WOOD STRUCTURE AND APPEARANCE
2/2
4
LESSON 1: Wood properties, its limitations and wood construction physics
Wood defects and faults
live knot | dead knot | knot with bark | rotten knot | edge knot | Wedge knot | leafy knot | group of knots
Macroscopic/microscopic
views of reaction wood
Related board defects
Standing tree (pine and spruce)
Types of knots
Hodley R.B. Understanding Wood: A Craftsman's Guide to Wood Technology. 2000
https://20d54786-a-62cb3a1a-s-sites.googlegroups.com/site/leonardoguitarresearch/glossary/Eng%20-%20Deformations.png?attachauth=ANoY7cpapMBSW-3jG8m2jTfvC0iWvOV2qhpRFY_6NjGeyQ5k9rnYg7qjkoj6p7ElcN3HaESI3-yCK9ZVQ-blXo_CeNBUmtt8TG-OSd3CbYG5ygBmqDLpz_3sy2ED1R4tNuMOPe0pjeUr8V82WpbNzWs6q_RP7iJ95pFDwuFXNibm_sE1-hsmLKqeKHr1AtS03ymwZvOPvIA51S0ZBoZNLJkgTklHStCakbNZS18oGgCPxu1uYCffzXRks-zjdcuNxPOtH9r7GCMq&attredirects=0
Wood Handbook, 2010

## Slide 5
PHYSICAL PROPERTIES
5
LESSON 1: Wood properties, its limitations and wood construction physics
Moisture content (MC) and density
https://www.wooduchoose.com/BlogPost/?Moisture-Content-of-Wood
https://www.reddit.com/r/Damnthatsinteresting/comments/fbhmw1/the_difference_in_density_in_wood_from_1918_to/
Wood Handbook, Robert J. Ross. Forest Products Laboratory USDA Forest Service. 2010, https://www.fs.usda.gov/treesearch/pubs/37440
Liepiņš J. Methodology development for forest stand biomass and carbon stock estimates in Latvia, doctoral thesis, LLU, 2019., 60 p.

## Slide 6
6
LESSON 1: Wood properties, its limitations and wood construction physics
MECHANICAL PROPERTIES
6
LESSON 1: Wood properties, its limitations and wood construction physics
F- load, N;
a – sample cross section width, mm;
l – sample cross section length, mm.
COMPRESSION
BENDING
TENSION
SHEAR
F – max. load, N;
l – span, mm;
b - width of the sample, mm;
h - thickness of the sample, mm;
F - load difference at elastic deformation, N;
f - displacement difference at elastic deformation, mm;
Wood Species | Bending strength, N mm-2 |  | Compression strength parallel to grain, N mm-2 |  | Compression strength perpendicular to grain, N mm-2 |  | Tension strength parallel to grain, N mm-2 |  | Density, kg m-3
 | MC 12% | MC 30% | MC 12% | MC 30% | MC 12% | MC 30% | MC 12% | MC 30% | 
Pine | 91 | 49 | 50 | 21 | 7,0 | 5,0 | 95 | 78 | 540
Spruce | 87 | 43 | 39 | 19 | 5,3 | 3,8 | 116 | 77 | 470
Oak | 103 | 66 | 57 | 31 | 10,2 | 7,2 | 140 | 107 | 820
https://extension.okstate.edu/fact-sheets/strength-properties-of-wood-for-practical-applications.html
https://www.buildup.eu/en/practices/cases/lifecycle-tower-one-building
https://inhabitat.com/lifecycle-tower-in-austria-will-be-worlds-tallest-wooden-building/new-25-8/
https://nptel.ac.in/content/storage2/courses/101104010/lecture39/39_6.htm
Xu M., Cui Z., Chen Z. and Xiang J. Experimental study on compressive and tensile properties of a bamboo scrimber at elevated temperatures. Construction and Building Materials, Volume 151, 2017
Gupta and Sinha. Effect of grain angle on shear strength of Douglas-fir wood. 2012.
PROPERTIES OVERVIEW
VISCOELASTICITY (click on the picture)

## Slide 7
TECHNOLOGICAL PROPERTIES
7
LESSON 1: Wood properties, its limitations and wood construction physics
saw-frame sawing | bend-saw sawing | ripsaw sawing | milling machine used
SAWN MATERIALS
SAWING TYPES
WOOD DRYING
https://www.woodcraft.com/blog_entries/how-to-air-dry-lumber-turn-freshly-cut-stock-into-a-cash-crop-of-woodworking-woods#
https://www.incomac.com/en/prodotti/pal-wood-dryer/

## Slide 8
OPERATIONAL PROPERTIES
8
LESSON 1: Wood properties, its limitations and wood construction physics
Wood Species | Hardness, N mm-2 | Density, kg m-3
 | MC 12% | 
Pine | 29/14 | 540
Spruce | 26/12 | 470
Oak | 68/40 | 820
ABRASION RESISTANCE OF WOOD
(click on picture)
https://catas.com/en-GB/news/the-abrasion-resistance-test
https://www.iml-service.com/sound-velocity-measurement/
https://www.swedishwood.com/wood-facts/about-wood/from-log-to-plank/properties-of-softwood/
https://na.pergo.com/
THERMAL CHARACTERISTICS
HARDNESS OF WOOD
SOUND VELOCITY
(click on picture)
For example PERGO®
SOME WOODEN PRODUCT TESTING
(click on picture)

## Slide 9
Limitations:
Not always, sometimes national laws do not allow to build up multi story houses.
Sometimes citizens have some prejudices – wooden houses burn, are not sustainable etc.
LESSON 1: Wood properties, its limitations and wood construction physics
In fact, usually we do not have enough knowledge to build up such wooden houses.
JUST SOME SMART EXAMPLES (click on the pictures)
From LATVIA
From AUSTRIA
From GREECE
From SPAIN
From FINLAND

## Slide 10
Benefits + or Disadvantages -
ARCHITECHTS +
Presentations are communication tools that can be demonstrations, lectures, speeches, reports, and more.
ENVIROMNENT and HEALTH +
Natural, renewable, CO2 neutral and recyclable material
CIVIL ENGINEERS -
Not friendly material for design (properties in all directions are various)
COSTS -
Not always the cheapest building material compete with structural steel or concrete
LESSON 1: Wood properties, its limitations and wood construction physics

## Slide 11
Future vision
(click on following buildings)
11
LESSON 1: Wood properties, its limitations and wood construction physics
https://www.creebuildings.com/project/life-cycle-tower-one
https://www.thinkwood.com
PAST
NOWADAYS
FUTURE

## Slide 12
QUESTIONS AND ANSWERS
12
LESSON 1: Wood properties, its limitations and wood construction physics
  1. What are the main sections of the pine trunk?
A: lower trunk part without knots; middle trunk part with dead knots; upper trunk part with live knots
2. What components of the trunk are visible in its cross section (mention at least 3 of them?
A: bark; pith; sapwood; heartwood; growth-annual rings; early wood; late wood
  3. What chemical elements are in wood?
A: carbon (C), hydrogen (H), oxygen (O) and nitrogen (N)
  4. What is wood moisture content (MC)?
A: It is water content in the wood, calculated in percentage
  5. What kind methods of determination of the wood moisture content (MC) do You know?
A: Electric moisture method; oven dry method; hygrometric method and distillation method
  6. What is wood shrinkage and swelling in which direction is the greatest one?
A: Changes of dimensions, in tangential
  7. What is the density of wood, units? Why determine the standard density at 12?
A: It is mass of wood peace divided by its volume, kg m-3. Just to compare the density between wood species
  8. What is the strength of the wood?
A: Maximum force which can be applied to the exact material
  9. In which direction is the strength greater?
A: In direction of wood fiber (parallel to fiber direction)
  10. What types of branches can be found on sawn timber surface?
A: live knot; dead knot; knot with bark; rotten knot; edge knot; wedge knot; leafy knot; group of knots
  11. How do the knots affect the strength and quality of wood?
A: Group of knots decrease strength of knots
  12. What are the timber defects for standing tree?
A: juvenile wood, reaction wood and slope of grain

## Slide 13
References
JOURNALS AND PUBLICATIONS
EN 13183-1:2002 Moisture content of a piece of sawn timber. Determination by oven dry method.
EN 13183-2:2002 Moisture content of a piece of sawn timber. Estimation by electrical resistance method.
EN 13183-3:2005 Moisture content of a piece of sawn timber. Estimation by capacitance method.
Gupta and Sinha. Effect of grain angle on shear strength of Douglas-fir wood. 2012., DOI:10.1515/hf-2011-0031Hoadley R.B. Understanding wood. The Taunton Press, China, 2000., 280 p.
Hodley R.B. Understanding Wood: A Craftsman's Guide to Wood Technology. The Taunton Press; 1st edition, 2000., 288 p.
Liepiņš J. Methodology development for forest stand biomass and carbon stock estimates in Latvia, doctoral thesis, LLU, 2019., 60 p.
Softwood sawn material application. Guidelines. (Skujkoku zāģmateriālu pielietošana. Vadlīnijas. In Latvian). 2009., ISBN/ISMN 978-9984-39-720-7.
Theapparat Y., Chandumpai A. and Faroongsarng D. Physicochemistry and Utilization of Wood Vinegar from Carbonization of Tropical Biomass Waste. DOI: 10.5772/intechopen.77380
Wertheimer D. Moisture & Wood Movement. How To & Calculators, 2019., https://www.branchingoutwood.com/blog/wood-movement-and-moisture.
Wood Handbook, Robert J. Ross. Forest Products Laboratory USDA Forest Service. 2010, https://www.fs.usda.gov/treesearch/pubs/37440
Xu M., Cui Z., Chen Z. and Xiang J. Experimental study on compressive and tensile properties of a bamboo scrimber at elevated temperatures. Construction and Building Materials, Volume 151, 2017, pp. 732-741.
13
LESSON 1: Wood properties, its limitations and wood construction physics